The Cleavage of Organosiloxanes with Dimethyl Carbonate: A Mild Approach to Graft-To-Surface Modification

Iryna Protsaka,d,e, Ian M. Hendersonb, Valentyn Tertykhc, Wen Donga,e*, Zi-Chun Led

a College of Environment, Zhejiang University of Technology, Hangzhou 310023, China

b Omphalos Bioscience, LLC, Albuquerque, NM, USA 87110

c Chuiko Institute of Surface Chemistry of National Academy of Sciences of Ukraine, 03164 Kiev, Ukraine

d College of Science, Zhejiang University of Technology, Hangzhou 310023, China

e Key Laboratory of Microbial Technology for Industrial Pollution Control of Zhejiang Province, Hangzhou, 310014, China

*Corresponding author: Wen Dong

E-mail address: dongwen@zjut.edu.cn

Tel: +86 571 88871576

Viscosity measurements S1. Depolymerization was performed with the use of 99.8 % ethanol solution. The polymer solution efflux time was measured with the use of a stopwatch by means of VPG–1 viscometer with the internal capillary diameter of 2.10 mm. Kinematic viscosity of the solution (η, m2/s) was calculated using the formula:

η = k×g×τ9.807,    		                               		(1)

where k – the viscometer constant that equaled 0.825 mm2/sec2, g  free-fall acceleration corresponding to 9.807 m/sec2 and τ  efflux time time, sec.

Figure S2. Apparatus for synthesis of high disperse materials with high content of the grafted organic groups: 1 – glass reactor, 2,7 – heating mantle, 3 – stirrer, 4 – glass stopper, 5 – glass laboratory thermometer, 6 – container mixing modifying reagent, 8 – batcher, 9 – injection system, 10 – inert gas cylinder, 11 – inert gas valve.

Equation S3. The modification degree (Θ) of the silica surface was estimated from the ratio of the optical density of a band of free silanols at 3742 cm-1 of modified and unmodified silicas:

θ=100 (1-DDo),          	                                                  (2)

where Do and D are the optical density of the mentioned band of the unmodified and modified silicas, respectively.

Equation S4. The apparent bonding density of the attached layers was calculated using the formula 3:

ρ = 6×105 (% C)1200×nc-Mw×(% C)1S(BET),		                  		(3)

where MW is the molecular weight of the methylphenylsiloxy group (131 g/mol), % C is the carbon weight percentage of the modified silica, and S(BET) is the surface area of the original silica (m2/g), nc is a number of carbon atoms in the grafted group. Equation 3 gives the number of [-Si(CH3C6H5)O-] repeat units per 1 nm2 of the surface (ρ).

Figure S5. 90 MHz 1H NMR spectrum of neat PDMS–100; the inset shows the methyl group shifts of parent PDMS–100.

Equation S6. Typically we conducted End-Group Analysis using formula of total siloxane repeats (Rt) (1) and formula of number of monomers per chain (N) (2). Total siloxane repeats (Rt) was calculated using the formula:

Rt=NMR signal for PDMS-100existing end groups ×protons per repeats       				   (1)

Number of monomers per chain (N) was calculated using the formula:

N=RtNe,             		                                                                   (2)

where Ne – number of end groups which was calculated using 1H NMR integration data, NE= (Nmethoxy + Nethoxy).

Figure S7. 90 MHz 1H NMR spectrum of depolymerizied PMPS; the inset shows the alkoxy groups shifts of depolymerized PMPS at 200 °C.

Figure S8. 13C CP/MAS NMR spectra of silica modified with neat PMPS and their mixture with DMC (1.8 mmol) at 200 °C for 2 h; the inset shows shifts of the grafted organic groups for both samples.

| ## a | ## b |
| --- | --- |
| Figure S9. Contact angle of SiO2 nanoparticles, modified with mixture of PMPS/DMC at 200 °C for 2 h (a) and photograph showing hydrophobic properties of SiO2/PMPS+DMC (b, 1) and unreacted SiO2 nanoparticles (b, 2). |  |