Fe3O4-Embedded and N-Doped Hierarchically Porous Carbon Nanospheres as High-Performance Lithium Ion Battery anodes

Jiayi Mao,a Dechao Niu*,a, Guangyu Jiang,a Nan Zheng,a Wenru Zhao,a Jianlin Shi, b Yongsheng Li*,a

a Lab of Low-Dimensional Materials Chemistry, Key Laboratory for Ultrafine Materials of Ministry of Education, School of Materials Science and Engineering, East China University of Science and Technology, Shanghai 200237, China.

b State Key Laboratory of High Performance Ceramics and Superfine Microstructure, Shanghai Institute of Ceramics, Chinese Academy of Sciences, Shanghai 200050, China

*Corresponding Authors

E-mail: dcniu@ecust.edu.cn (Dechao Niu), ysli@ecust.edu.cn (Yongsheng Li)

Number of pages: 10 (Page S1-S10)

Number of figures: 10 (Figure S1- S10)

Number of tables: 3 (Table S1-S3)

Figure S1. TEM images of the monodispersed, 6 nm sized Fe3O4 nanoparticles.

Figure S2. SEM images of Fe3O4@N-HPCNs

Figure S3. TEM images of N-HPCNs at different magnifications

Figure S4. N2 adsorption/desorption isotherms of Fe3O4@N-HPCNs and N-HPCNs

Figure S5. The EDS spectra of various elements for Fe3O4@N-HPCNs before (a) and after (b) the etching process.

Table S1. The BET surface areas, pore volumes and pore size distributions of Fe3O4@N-HPCNs and N-HPCNs.

| Samples | Specific surface area (m2 g-1) | t-Plot micropore area (m2 g-1) | Pore volume (cm3 g-1) | Pore size (nm) |
| --- | --- | --- | --- | --- |
| Fe3O4@N-HPCNs | 688.6 | 134.7 | 0.92 | 2.7&15.8 |
| N-HPCNs | 814.2 | 158.3 | 1.13 | 2.9&16.1 |

Figure S6. CV curves of the Fe3O4 anode.

Figure S7. CV curves of the N-HPCNs anode.

Figure S8. Cycling performance of Fe3O4@N-HPCNs 0.5 A g-1.

Figure S9. Cycling performances of N-HPCNs and Fe3O4 at 1 A g-1.

Table S2. Impedance Parameter Values Obtained by the Fitting of the Nyquist Plots in Figure 7b.

| Samples | Re (Ω) | Rct (Ω) | CPE (μF) | Zw (Ω) |
| --- | --- | --- | --- | --- |
| Before cycling | 1.676 | 90.34 | 14.93 | 30.45 |
| 20th cycle | 6.863 | 178.83 | 86.64 | 67.09 |
| 100th cycle | 2.918 | 98.53 | 227 | 11.51 |

Figure S10. TEM image of the Fe3O4@N-HPCNs anode after 250 cycles.

Table S3. Comparison of the performances and Fe3O4 contents of various Fe3O4-based materials for LIBs reported in the literatures.

| Fe3O4-based materials | Capacity (mAh g-1) at different current density | Fe3O4 content (wt%) | Ref. |
| --- | --- | --- | --- |
| Fe3O4@ N-HPCNs | ~1240 (100 cycles) at 0.1 A g-1 ~581 (400 cycles) at 1 A g-1 | ~20.12 | This work |
| Hollow N-doped Fe3O4/Carbon Nanocages | ~700 (100 cycles) at 0.2 A g-1 | ~70.13 | [1] |
| Fe3O4@C Nanoparticles | ~800 (100 cycles) at 0.1 A g-1 ~530 (350 cycles) at 1 A g-1 | ~89.1 | [2] |
| Fe3O4@C yolk-shelled Nanocubes | ~1100 (50 cycles) at 0.1 A g-1 | ~92.48 | [3] |
| G- Fe3O4-GNRs | ~787 (55 cycles) at 0.1 A g-1 | ~60 | [4] |
| Sandwich-Structured Graphene- Fe3O4@C | ~1200 (150 cycles) at 0.1 A g-1 | ~73.5 | [5] |
| 3D Fe3O4/macroporous Graphene | ~712 (180 cycles) at 0.1 A g-1 | ~56.8 | [6] |
| Fe3O4/N-doped Carbon/Nitrogen-doped Graphene | ~905 (100 cycles) at 0.2 A g-1 | ~58.3 | [7] |
| Fe3O4@C Nanoparticles | ~1290(200 cycles) at 0.1 A g-1 ~520 (200 cycles) at 1 A g-1 | ~30 | [8] |
| Fe3O4@PPy Nanocages | ~950 (100 cycles) at 0.2 A g-1 | ~88.7 | [9] |
| Fe3O4-Fe @ Bamboo-like Carbon Nanotubes | ~764 (100 cycles) at 0.3 A g-1 | ~34 | [10] |
| Fe3O4/C Composite | ~1300 (100 cycles) at 0.1 A g-1 | ~67 | [11] |

References

(1) Wang, L.; Wu, J.; Chen, Y.; Wang, X.; Zhou, R.; Chen, S.; Guo, Q.; Hou, H.; Song, Y., Hollow Nitrogen-doped Fe3O4/Carbon Nanocages with Hierarchical Porosities as Anode Materials for Lithium-ion Batteries. Electrochim. Acta 2015, 186, 50-57, DOI 10.1016/j.electacta.2015.10.134.

(2) Ma, C.; Shi, J.; Zhao, Y.; Song, N.-j.; Wang, Y., A novel porous reduced microcrystalline graphene oxide supported Fe3O4@C nanoparticle composite as anode material with excellent lithium storage performances. CHEM. ENG. J. 2017, 326, 507-517, DOI 10.1016/j.cej.2017.05.180.

(3) Liu, Z.; Yu, X.-Y.; Paik, U., Etching-in-a-Box: A Novel Strategy to Synthesize Unique Yolk-Shelled Fe3O4@Carbon with an Ultralong Cycling Life for Lithium Storage. Adv. Energy Mater. 2016, 6 (6), 1502318, DOI 10.1002/aenm.201502318.

(4) Li, L.; Kovalchuk, A.; Fei, H.; Peng, Z.; Li, Y.; Kim, N. D.; Xiang, C.; Yang, Y.; Ruan, G.; Tour, J. M., Enhanced Cycling Stability of Lithium-Ion Batteries Using Graphene-Wrapped Fe3O4-Graphene Nanoribbons as Anode Materials. Adv. Energy Mater. 2015, 5 (14), 1500171, DOI 10.1002/aenm.201500171.

(5) Zhao, L.; Gao, M.; Yue, W.; Jiang, Y.; Wang, Y.; Ren, Y.; Hu, F., Sandwich-Structured Graphene-Fe3O4@Carbon Nanocomposites for High-Performance Lithium-Ion Batteries. ACS Appl. Mater. Interfaces 2015, 7 (18), 9709-9715, DOI 10.1021/acsami.5b01503.

(6) Lu, X.; Wang, R.; Bai, Y.; Chen, J.; Sun, J., Facile preparation of a three-dimensional Fe3O4/macroporous graphene composite for high-performance Li storage. J. Mater. Chem. A 2015, 3, 12031–12037, DOI 10.1039/c5ta01803j.

(7) Luo, H.; Ji, D.; Yang, Z.; Huang, Y.; Xiong, G.; Zhu, Y.; Guo, R.; Wan, Y., An ultralight and highly compressible anode for Li-ion batteries constructed from nitrogen-doped carbon enwrapped Fe3O4 nanoparticles confined in a porous 3D nitrogen-doped graphene network. Chem. Eng. J. 2017, 326, 151-161, DOI 10.1016/j.cej.2017.05.102.

(8) He, Z.; Wang, K.; Zhu, S.; Huang, L. A.; Chen, M.; Guo, J.; Pei, S.; Shao, H.; Wang, J., MOF-Derived Hierarchical MnO-Doped Fe3O4@C Composite Nanospheres with Enhanced Lithium Storage. ACS Appl. Mater. Interfaces 2018, 10 (13), 10974-10985, DOI 10.1021/acsami.8b01358.

(9) Liu, J.; Xu, X.; Hu, R.; Yang, L.; Zhu, M., Uniform Hierarchical Fe3O4@Polypyrrole Nanocages for Superior Lithium Ion Battery Anodes. Adv. Energy Mater. 2016, 6 (13), 1600256, DOI 10.1002/aenm.201600256.

(10) Du, L.; Xu, C.; Liu, J.; Lan, Y.; Chen, P., One-step detonation-assisted synthesis of Fe3O4-Fe@BCNT composite towards high performance lithium-ion batteries. Nanoscale 2017, 9 (38), 14376-14384, DOI 10.1039/c7nr05362b.

(11) Yang, Z.; Su, D.; Yang, J.; Wang, J., Fe3O4/C composite with hollow spheres in porous 3D-nanostructure as anode material for the lithium-ion batteries. J. Power Sources 2017, 363, 161-167, DOI 10.1016/j.jpowsour.2017.07.080.