Supplementary material for:

White light emission from a zero-dimensional lead-chloride hybrid material

S. Elleuch,1,* A. Lusson,2 S. Pillet,3 K. Boukheddaden2 and Y. Abid1

1Laboratoire de Physique Appliquée, Faculté des Sciences de Sfax, Route de Soukra km 3.5 BP 1171, 3018 Sfax, Tunisia.

2Groupe d’Etudes de la Matière Condensée (GEMaC), UMR-CNRS 8653, Université de Versailles Saint Quentin En Yvelines, Université Paris-Saclay, 45 Avenue des Etats-Unis, 78035 Versailles, France.

3Laboratoire de Cristallographie, Résonance Magnétique et Modélisations, UMR-CNRS 7036, Institut Jean Barriol, Université de Lorraine, BP 239, 54506 Vandœuvre-lès-Nancy, France.

*Corresponding author : slimlpa@yahoo.fr

Table S1. Crystallographic data for (TAE)2[Pb2Cl10](Cl)2.

| Chemical formula | (C6N4H22)2[Pb2Cl10]Cl2 |
| --- | --- |
| Chemical formula moiety | Cl10 Pb2, 2(C6 H22 N4), 2(Cl) |
| Formula weight/gmol-1 | 1140.33 |
| Crystalsystem | triclinic |
| Space group | P-1 |
| a/Å | 9.9851(10) |
| b/Å | 10.2719(10) |
| c/Å | 18.4551(17) |
| α/° | 74.596(3) |
| β/° | 85.797(4) |
| γ/° | 67.643(3) |
| Volume/Å3 | 1686.9(3) |
| Z | 2 |
| Temperature (K) | 100(2) |
| Collected reflections | 177910 |
| θmin-θmax/° | 2.206-36.418 |
| Crystal colour | colourless |
| F(000) | 1080 |
| Absorption coefficient | 10.938 |
| Radiation source (wavelength) | MoK\a (0.71073) |
| hmin- hmax; kmin-kmax; lmin-lmax/° | -16-16 ; -17-17 ; -30-30 |
| Rint | 0.0556 |
| aR1 [F2> 2*s(F2)] | 0.0306 [0.0219] |
| awR2 [F2> 2*s(F2)] | 0.0526 [0.0454] |
| bGoodness-of-fit on F2 | 1.154 |
| Largest diff. peak/hole / e- Å-3 | 1.291 / -1.604 |

aR1=Σ(Fo-Fc|/Fo) and wR2= {Σ[w(Fo2-Fc2)2]/ Σ[w(Fo2)2]}1/2

bG.O.F = [(Σ(w(Fo2-Fc2))2/(Nobs-Nvar)]1/2

Table S2. Experimental bond lengths and angles of the two [Pb2Cl10]6- groups.

| Bond | Length (Å) | Angle | Value (°) |
| --- | --- | --- | --- |
| Pb1-Cl4 | 2.7724(5) | Cl4-Pb1-Cl3 | 87.252(16) |
| Pb1-Cl3 | 2.7840(5) | Cl4-Pb1-Cl5 | 83.671(14) |
| Pb1-Cl5 | 2.9078(6) | Cl3-Pb1-Cl5 | 87.174(15) |
| Pb1-Cl1 | 2.9345(5) | Cl4-Pb1-Cl1 | 170.175(14) |
| Pb1-Cl2 | 2.9599(6) | Cl3-Pb1-Cl1 | 91.010(15) |
| Pb1-Cl5 | 3.0488(5) | Cl5-Pb1-Cl1 | 86.587(14) |
| Pb2-Cl7 | 2.7835(5) | Cl4-Pb1-Cl2 | 88.480(15) |
| Pb2-Cl9 | 2.8406(5) | Cl3-Pb1-Cl2 | 95.037(15) |
| Pb2-Cl8 | 2.8624(5) | Cl5-Pb1-Cl2 | 171.740(14) |
| Pb2-Cl10 | 2.9397(6) | Cl1-Pb1-Cl2 | 101.309(15) |
| Pb2-Cl6 | 2.9523(6) | Cl4-Pb1-Cl5 | 97.068(15) |
| Pb2-Cl9 | 3.0430(6) | Cl3-Pb1-Cl5 | 174.998(14) |
|  |  | Cl5-Pb1-Cl5 | 90.787(14) |
|  |  | Cl1-Pb1-Cl5 | 84.306(15) |
|  |  | Cl2-Pb1-Cl5 | 87.622(14) |
|  |  | Cl7-Pb2-Cl9 | 91.798(16) |
|  |  | Cl7-Pb2-Cl8 | 90.723(15) |
|  |  | Cl9-Pb2-Cl8 | 83.934(15) |
|  |  | Cl7-Pb2-Cl10 | 88.353(15) |
|  |  | Cl9-Pb2-Cl10 | 91.501(15) |
|  |  | Cl8-Pb2-Cl10 | 175.313(14) |
|  |  | Cl7-Pb2-Cl6 | 91.297(15) |
|  |  | Cl9-Pb2-Cl6 | 176.750(14) |
|  |  | Cl8-Pb2-Cl6 | 97.021(15) |
|  |  | Cl10-Pb2-Cl6 | 87.595(15) |
|  |  | Cl7-Pb2-Cl9 | 166.464(14) |
|  |  | Cl9-Pb2-Cl9 | 89.539(15) |
|  |  | Cl8-Pb2-Cl9 | 76.021(15) |
|  |  | Cl10-Pb2-Cl9 | 105.081(15) |
|  |  | Cl6-Pb2-Cl9 | 87.684(15) |
|  |  | Pb1-Cl5-Pb1 | 89.213(14) |
|  |  | Pb2-Cl9-Pb2 | 90.461(15) |

Figure S1.Crystal structure of the (TAE)2[Pb2Cl10](Cl)2 projected along the (left) a-axis and (right) c-axis.

Figure S2. N-H…Cl hydrogen bonds in (TAE)2[Pb2Cl10](Cl)2. The two symmetry independent [TAE]4+ cations are involved in a dense network of N-H…Cl hydrogen bonds.(left) The first cation is connected to four [Pb2Cl10]6- groups and 2 Cl- ions; (right) the second cation is connected to five [Pb2Cl10]6- groups and 2 Cl- ions.

Figure S3. Structural distortion of the two [Pb2Cl10]6- groups. The geometries of the two [Pb2Cl10]6- groups is quite different

86.03(2)°

Pb1

81.36(2)°

Pb2

78.71(2)°

99.24(2)°

Figure S4. Superposition of the two [Pb2Cl10]6- groups.

Pb1

Pb2

Figure S5. Superposition of the [TAE]4+ cations. The two [TAE]4+ adopt the same conformation

Figure S6. Room temperature Raman spectrum of (TAE)2[Pb2Cl10](Cl)2.