Supporting Information

Reaction of Water Stable C60 Aggregates with Ozone

John D. Fortner1, Doo-Il Kim1, Adina M. Boyd2, Joshua C. Falkner2, Sean Moran3,Vicki L. Colvin2, Joseph B. Hughes1, and Jae-Hong Kim1*

1 School of Civil and Environmental Engineering, Georgia Institute of Technology, Atlanta, GA  30332

2 Department of Chemistry, Rice University, Houston, TX 77005

3 Department of Biochemistry and Cell Biology, Rice University, Houston, TX 77005

Authors’ Email Addresses (in order): john.fortner@gatech.edu; gtg722i@mail.gatech.edu; aboyd@rice.edu; jfalkner@rice.edu; smoran@rice.edu; colvin@rice.edu; joseph.hughes@ce.gatech.edu; jaehong.kim@ce.gatech.edu

*Corresponding author. E-mail: jaehong.kim@ce.gatech.edu; phone: (404) 894-2265; fax: (404) 385-7087

Supporting information provides additional information in the form of one figure (S1) regarding UV-Vis spectral analysis (offset) of ozonated products over a range of pH values.  Additionally, UV-Vis spectrum (offset) of a commercial fullerene oxide (fullerol) from MER Corp. (Tucson, AZ) prepared through substitution of brominated C60 at pH 3 (C60(O)x(OH)y where x + y = ~22) over a similar range of pH values is provided for comparison.

Figure S1.  UV-Vis spectra (offset) of (A) ozonation product of nC60 (100 mg/L) at pH 3.4 (unadjusted), 7.4 and 11.4; nC60 provided at reference (B) commercial fullerol (40 mg/L) at pH 2.3, 4.6 (unadjusted), 7.4, and 11.4.

# Text boxes

A

B