Supporting Information on the paper

Complex Formation of DNA with Oppositely Charged Polyelectrolytes of Different Chain Topology: Cylindrical Brushes and Dendrimers

Dominic Störkle, Sabrina Duschner, Nils Heimann, Michael Maskos, Manfred Schmidt*

Institut für Physikalische Chemie, Universität Mainz, Jakob-Welder-Weg 11, D-55128 Mainz.

1.	Berry plot of pUC19-supercoiled DNA in 5 mM sodium phosphate buffer (pH 7)

Fig. S1: Berry plot of pUC19-supercoiled DNA in 5 mM sodium phosphate buffer (pH 7) obtained by static light scattering.

# 2.	Gel electrophoresis of the other DNA-polycation systems

Fig. S2a: Weight fraction of freely migrated DNA in DNA-PVP26 complex solutions.

Fig. S2b: Weight fraction of freely migrated DNA in DNA-PVP47 complex solutions.

Fig. S2c: Weight fraction of freely migrated DNA in DNA-PAMAM complex solutions.

# 3.	Composition of PVP47-DNA complex solutions with excess PVP47

The complexation experiments shown here were performed with excess PVP47 brushes to which pUC18-supercoiled DNA was added. pUC18-supercoiled DNA is identical to pUC19-supercoiled DNA used in the paper in terms of number of base pairs, molar mass and contour length.

The amount of uncomplexed PVP47-brushes in the complex solutions is determined by AFM and SEC. Fig. S.3a-c show the results obtained by simply counting the number of uncomplexed brush molecules on the AFM pictures, thus yielding w**DNA(AFM) = 0.33 ± 0.06 by linear extrapolation. SEC measurements (see Fig. S4a-b) of the identical complex solution lead w**DNA(SEC) = 0.33 ± 0.04 by linear extrapolation. Both values coincide much better than expected and indicate strongly that the assumptions discussed in main text are fulfilled.

Fig. S3a: AFM picture of the pure PVP47 brushes.

Fig. S3b: AFM picture of PVP47-DNA complexes with excess of PVP47 (wDNA = 0.22).

Fig. S3c: Number of uncomplexed brushes per complex and extrapolation to cPVP47,uncomplexed = 0, determined by statistical evaluation of the AFM-pictures.

Fig. S4a: SEC elution curves for uncomplexed PVP47 brush and complex solutions, normalized on equal PVP47 mass concentrations.

Fig. S4b: Integration of the PVP47 peak in the SEC eluograms (Fig. S.4a, elution volume 18 – 32 mL) and extrapolation to cPVP47,uncomplexed = 0.

# 3.	Effect of concentration of mixing

Fig. S5: Apparent molar mass of DNA-PVP26 complexes as function of weight fraction wDNA for various concentrations of mixing.